## Slide 1: (Semi-)Closed loop recycling of solid oxide cells 9th International Conference on Fundamentals & Development of Fuel Cells FDFC 2023
SEP 25th 2023 | S. Sarner | N.H. Menzler | O. Guillon
Forschungszentrum Jülich | Materials synthesis & Processing (IEK-1)

## Slide 2: H2 electrolyser development
[1] Hydrogen Insights Report September, Hydrogen Council, McKinsey & Company (2022).
[1]
Recycling targets: cost reduction, material preservation, decrease CO2-emissions
2025
H2 policy agreements Germany:
10 GW installed electrolyser capacity in 2030
H2Giga flagship project: Scale-up of electrolyser technologies
SOC market development:
SOC market share low until 2030 (~5%)
5% refers to 12 million SOC (10x10 Jülich design)
Critical raw materials in SOCs:
REEs, Nickel, Cobalt, Strontium

## Slide 3: SOC designs & Challenges
DBL, FE, (CL)
Metal-supported
Fuel electrode-supported
Electrolyte-supported
MS
CS
(CL), AE
AE, DBL, E, FE
FE, E, DBL, AE, (CL)
E
wt%
wt%
wt%

## Slide 4: FESC recycling concept
Fuel-side recycling
Air-side
recycling

## Slide 5: LSCF leaching
Acid type
Additive H2O2
Temperature
Time
Why H2O2?
increases solubility
reducing agent
oxidizing agent
NiO:
YSZ:
LSCF:
GDC:
53
39
6
1
wt%
Cell powder
Concentration: 2M (org.) 6M (inorg.)
Solid to Liquid:
1g/L
Notes: Y-Axis = Sum of all LSCF components
X-axis = different acid types
Cell powder

## Slide 6: LSCF leaching
<48%
~100%
~100%
<95%
<89%

## Slide 7: Nickel leaching
~34%

## Slide 8: Response surface Methodology
Concentration [%]
LSCF [wt%]
10
15
20
25
10
15
20
20
30
40
50
60
70
80
Temperature [°C]
Fraction completely dissolved
Sweet spot for LSCF leaching:
Leaching media: HCl
Concentration: 6M/~20%
Contact time: 2h
Solid/Liquid (S/L): 50g/L
US-stirred
LSCF [wt%]
Contact time

## Slide 9: Bulk cell material investigated
electrolyte
fuel electrode
barrier layer
air electrode
contact layer
[5] European Commission, Study on the Critical Raw Materials for the EU 2023, Publications Office of the European Union, DOI: 10.2873/725585.
Cell structure
YSZ
Ni-YSZ
GDC
LSCF
LCC10*
>85wt%
(fuel-side recycling)
<15wt%
(air-side recycling)
* La1Mn0.45Co0.35Cu0.2O3-δ

## Slide 10: Powder preparation
Cumulative fraction [%]
Diameter [µm]
Relative fraction [%]
Milling study via tumble mixing
*EoL End-of-Life
**CT/J CeramTec/Jülich cells
*
*
**

## Slide 11: Tape casting
Viscosity
Green tapes

## Slide 12: Substrate shrinkage & Porosity
Shrinkage decreasing (linear) ↓ ; Porosity increasing (non-linear, max. Δφ = 9.6%) ↑
Grain shape & nickel distribution comparable to standard, no visible defects
Shrinkage
*
* pre-study by M. Hilger (master‘s thesis, 2022)
Porosity (ox. substrates)

## Slide 13: Mechanical stability of substrate
Ring-on-ring set up (FZJ, IEK-2):
Room temperature
100 N min-1
20 samples per series
Results:
Fracture strength Ox. > Red.
Weibull modulus 5.8–8.5

## Slide 14: Take home messages
Separation of oxygen-electrode via mineral acids (HCl/HNO3)
Reprocessing to new substrate possible by adjusting particle size & specific surface area
Predictable changes in shrinkage & porosity with increasing recycled content
Mechanical stability slightly lower for recycled samples
(LSCF precursor recovery via oxalate precipitation)
OUTLOOK
11/12 manufactured full cells survived without defects!
Leakage test succesful
Single cell testing @FZJ; IEK-9 (currently performed)

## Slide 15: Thank you for your attention 9th International Conference on Fundamentals & Development of Fuel Cells
SEP 25th 2023 | S. Sarner | N.H. Menzler | O. Guillon
Collaboration:
N. Wettengl (ZEA-3, FZJ)
T. Osipova (IEK-2, FZJ)
J. Malzbender (IEK-2, FZJ)
ACKNOWLEDGEMENTS
Supervision:
O. Guillon
N.H. Menzler