### Divalent cation contributions to the co-transport of functionalized multi-walled carbon nanotubes in porous media in the presence of bentonite or goethite nanoparticles: Experiment and simulation

Miaoyue Zhanga, b, Scott A. Bradfordc, Erwin Klumppd, Jiří Šimůneke, Yijun Moa, Kengbo Dinga, Quan Wanb, f, Shizhong Wanga, Chao Jina, b*, and Rongliang Qiua, b, f*

School of Environmental Science and Engineering, Guangdong Provincial Key Laboratory of Environmental Pollution Control and Remediation Technology, Sun Yat-sen University, Guangzhou 510006, P.R. China

bGuangdong Laboratory for Lingnan Modern Agriculture, Guangzhou 510642, China

cUSDA, ARS, Sustainable Agricultural Water Systems (SAWS) Unit, 239 Hopkins Road, UC Davis, Davis, CA 95616, USA

dAgrosphere Institute (IBG-3), Forschungszentrum Jülich GmbH, 52425 Jülich, Germany

eDepartment of Environmental Sciences, University of California Riverside, Riverside, CA 92521, USA

fGuangdong Provincial Key Laboratory of Agricultural & Rural Pollution Abatement and Environmental Safety, College of Natural Resources and Environment, South China Agricultural University, Guangzhou 510642, China

Revision submitted to

Journal of Hydrology

June, 2023

*Corresponding author:

Chao Jin: jinchao3@mail.sysu.edu.cn;

Rongliang Qiu: eesqrl@mail.sysu.edu.cn;

Pages: 17

Tables: 3

Figures: 7

Introduction

The supporting information contains details about interaction energy calculations (S1), batch experiments (S2), molecular dynamics (MD) simulations (S3), and numerical modeling (S4). Table S1 shows the zeta potentials and hydrodynamic diameters of MWCNTs, BNPs, GNPs, MWCNTs-BNPs, and MWCNTs-GNPs in 1 mM CaCl2. Table S2 shows other fitted parameters based on M1, M2, and M3 models. Table S3 shows the standard error coefficients of fitted model parameters. Figures S1 and S2 show the observed and fitted (M2 and M3 models, respectively) BTCs and RPs in the column experiments. Figure S3 presents plots of the dimensionless interaction energy as a function of the separation distance (h) when a spherical colloid, with properties similar to MWCNTs in QS at the ionic strength of 1 mM KCl or CaCl2 in the presence or absence of BNPs or GNPs. Figure S4 shows the results of batch experiments.

S1 - Interaction Energy Calculations

The approach of Bradford and Torkzaban (Bradford and Torkzaban, 2013) was used to calculate the total interaction energy (Φ) of a spherical colloid with similar properties to MWCNTs in the presence of various concentrations of BNPs or GNPs. The value of Φ for a spherical colloid and collector system was considered to be the sum of electrostatic, van der Waals, and Born repulsion interaction energies:

Φh=Φelh+ΦvdWh+ΦBornh						[S1]

where Φ [ML2T-2] is the interaction energy on the underlying smooth surface, h [L] is the separation distance from the center of the electrostatic zone, Φel [ML2T-2], ΦvdW [ML2T-2], and ΦBorn [ML2T-2] are the electrostatic, van der Waals, and Born interaction energies on the smooth surface, respectively. The value of Φel was determined using the constant surface potential interaction expression of Hogg et al. (1966) for a sphere-plate interaction as:

Φelh=πεε0rc2ζ1ζ2ln1+exp⁡(-κh)1-exp⁡(-κh)+ζ12+ζ22ln1-exp⁡(-2κh)	[S2]

where  (dimensionless) is the dielectric constant of the medium, 0 [M−1L−3T4A−2, where A denotes ampere] is the permittivity in a vacuum, rc [L] is the radius of a colloid, ζ1 is the zeta potential of the colloid, ζ1 is the zeta potential of the collector, and κ [L−1] is the Debye-Huckel parameter. The value of ΦvdW for a sphere-plate interaction was determined using the expression by Gregory (1981) as:
ΦvdWh=-A123rc6h1+14hλ-1							[S3]

where A123 [ML2T−2 is the combined Hamaker constant, and λ is a characteristic wavelength that was taken as 100 nm (Bendersky and Davis, 2011). The value of ΦBorn was calculated from Ruckenstein and Prieve (1976) as:

ΦBornh=A123σc675608rc+h(2rc+7)7+6rc-hh7							[S4]

The collision diameter,σc, was taken as 0.26 nm in order to achieve a primary minimum depth at 0.157 nm, a commonly accepted distance of the closest approach (Elimelech et al., 1998). All interaction energies were made dimensionless by dividing by the product of the Boltzmann constant (kB =1.38×10−23 J K−1) and the absolute temperature (TK).

S2 – Batch experiments

The adsorption of MWCNTs on BNPs or GNPs was conducted as follows: 15 ml of MWCNT suspension with concentrations of 0 - 10 mg L-1 (at the ionic strength of 1 mM KCl or CaCl2) was added to 0.01 g BNPs or GNPs in 15 ml centrifuge tubes (pH ≈ 5.4). Mixtures were shaken using an over-head shaker for 24 h. Adsorption kinetic experiments indicated that the duration of 24 h was sufficient to achieve adsorption equilibrium. The tubes were then centrifugated (Allegra 64 R, Beckman Coulter) at 2000 rpm for 2 min. The unattached MWCNT, BNPs, or GNPs were measured in the supernatant by the UV-Vis spectrometer (230 nm) and ICP-MS to determine the concentrations of MWCNT and Fe. The calibration curves between absorbance and concentration for GNPs and BNPs at 230 nm were determined to eliminate the suspended BNPs and GNPs in the supernatant. Blank experiments with only MWCNTs suspension or only adsorbents of BNPs or GNPs were also conducted to verify the separation of individual particles (e.g., MWCNTs, BNPs-MWCNTs, or GNPs-MWCNTs). Results indicated that little GNPs and BNPs remained in the supernatant when the background solution was 1 mM KCl. Therefore, the centrifugation was efficient in individually separate MWCNTs, BNPs-MWCNTs, or GNPs-MWCNTs. All the batch experiments were performed in triplicate.

S3-Molecular Dynamics Simulations

Molecular dynamics (MD) simulations were carried out to investigate the mean distance between the centroids of MWCNTs and the binding energies between two nanoparticles (MWCNTs with BNPs or GNPs) in IS=1 mM CaCl2, which were based on a Charmm 36 force field (Soteras Gutierrez, 2016; Vanommeslaeghe, 2010) and performed using the Gromacs-4.6.7 software package (Polyakov et al., 2008). The time step was 2 fs, and the total run time was 10 ns NPT for the equilibrium MD simulation. We used the relaxed system as a starting configuration. Prior to system relaxation MD, energy minimization was carried out with a composite protocol of steepest descent using termination gradients of 100 . The Nose´-Hoover thermostat (Berendsen et al., 1984) was used to maintain the equilibrium temperature at 298 K and 1 bar, with periodic boundary conditions imposed on all three dimensions. The Particle Mesh-Ewald method (Astrakas et al., 2012; Essmann et al., 1995) was used to compute long-range electrostatics within a relative tolerance of 1x10-6. A cut-off distance of 1.2 nm was applied to real-space Ewald interactions. The same value was used for van der Waals interactions. The LINCS algorithm (Hess et al., 1997) was applied to constrain bond lengths of hydrogen atoms. A leap-frog algorithm (Wilfred et al., 1988) was used with a time step of 2 fs.

S4-Numerical modeling

HYDRUS-1D includes provisions for inverse parameter estimation using a nonlinear least squares optimization routine. The single-species transport of MWCNTs, BNPs, and GNPs was described with Equations [2-4] and [5-7] by setting ΓC and ΓS to zero, respectively. The M1 and M2 modeling approaches describe the single-species transport and co-transport of MWCNTs, BNPs, and GNPs, respectively. The transport and retention parameters (SCmax/Co, kaC, and kdC, or SSmax/Co, kaS, and kdS) for MWCNTs, BNPs, and GNPs data sets were independently determined using the M1 approach. The M2 approach allows for competitive blocking by fixing the retention and release parameters to those determined from M1 (SCmax/Co, kaC, and kdC, or SSmax/Co, kaS, and kdS), and then simultaneously optimizing values of ΓC and ΓS to both MWCNTs, BNPs and, GNPs data sets. The parameter ΓC accounts for differences in the cross-sectional areas of the particles and the porous medium surface that contributes to the retention of MWCNTs and natural nanoparticles (BNPs or GNPs). When SCmaxand SSmaxencompass the same area on the porous media surface, the value of ΓC=1/ΓS=AS/AC (Becker et al., 2015; Zhang et al., 2019), where AS [L2] and AC [L2] are the cross-sectional areas of the natural nanoparticles (BNPs or GNPs) and MWCNT, respectively. The M3 model considers only time-dependent (Langmuirian blocking) retention by fitting SCmax/Co, kaC, and kdC, or SSmax/Co, kaS, and kdS at a time.

References

Astrakas, L.G., Gousias, C. and Tzaphlidou, M., 2012. Structural destabilization of chignolin under the influence of oscillating electric fields. J. Appl. Phys.  111(7), 104-109.

Becker, M.D., Wang, Y., Pennell, K.D. and Abriola, L.M., 2015. A Multi-Constituent Site Blocking Model for Nanoparticle and Stabilizing Agent Transport in Porous Media. Environ. Sci.-Nano 2(2), 155-166.

Bendersky, M. and Davis, J.M., 2011. DLVO interaction of colloidal particles with topographically and chemically heterogeneous surfaces. J. Colloid Interf. Sci. 353(1), 87-97.

Berendsen, H.J.C.P., Postma, J., Gunsteren, W., Dinola, A.D. and Haak, J.R., 1984. Molecular-Dynamics with Coupling to An External Bath. J. Chem. Phys. 81, 3684.

Bradford, S.A. and Torkzaban, S., 2013. Colloid Interaction Energies for Physically and Chemically Heterogeneous Porous Media. Langmuir 29(11), 3668-3676.

Elimelech, M., Gregory, J., Jia, X. and Williams, R.A., 1998. Particle deposition and aggregation: measurement, modelling and simulation.

Essmann, U., Perera, L., Berkowitz, M.L., Darden, T., Lee, H. and Pedersen, L.G., 1995. A smooth particle mesh Ewald method. J. Chem. Phys. 103(19), 8577-8593.

Gregory, J., 1981. Approximate expressions for retarded van der Waals interaction. J. Colloid Interf. Sci. 83(1), 138-145.

Hess, B., Bekker, H., And, H. and Fraaije, J., 1997. LINCS: A linear constraint solver for molecular simulations. J. Comput. Chem. 18, (12), 1463-1472.

Hogg, R., Healy, T.W. and Fuerstenau, D., 1966. Mutual coagulation of colloidal dispersions. Trans. Faraday Soc. 62, 1638-1651.

Polyakov, N., Epifanovsky, E., Grigorenko, B.L., Krylov, A.I., Nemukhin, A.V. and Guidoni, L., 2009. Quantum chemical benchmark studies of the electronic properties of the green fluorescent protein chromophore: 2. cis-trans isomerization in water. J. Chem. Theory Comput. 5, (7), 1907-1914.

Ruckenstein, E. and Prieve, D.C., 1976. Adsorption and desorption of particles and their chromatographic separation. Aiche J. 22(2), 276-283.

Gutiérrez, I. S., Lin, F. Y., Vanommeslaeghe, K., Lemkul, J. A., Armacost, K. A., Brooks, C. L., MacKerell Jr., A. D., 2016. Parametrization of halogen bonds in the CHARMM general force field: improved treatment of ligand–protein interactions. Bioorgan. Med. Chem. 24, (20), 4812-4825.

Vanommeslaeghe, K.H., Hatcher, E., Acharya, C., Kundu, S., Zhong, S., Shim, J., Darian, E., Guvench, O., Lopes, P., Vorobyov, I., MacKerell Jr., A. D., 2010. CHARMM general force field: A force field for drug-like molecules compatible with the CHARMM all-atom additive biological force fields. J. Comput. Chem. 31, (4), 671-690.

van Gunsteren, W.F. and Berendsen, H., J., C., 1988. A leap-frog algorithm for stochastic dynamics. Mol. Simulat. 1.

Zhang, M., Bradford, S.A., Šimůnek, J., Vereecken, H. and Klumpp, E., 2019. Co-transport of multi-walled carbon nanotubes and sodium dodecylbenzenesulfonate in chemically heterogeneous porous media. Environ. Pollut. 247, 907-916.

Table S1. Hydrodynamic diameters of MWCNTs in the presence and absence of BNPs or GNPs in CaCl2 at an ionic strength of 1 mM (pH ≈ 5.4).

| Concentration of MWCNT [mg L-1] | Concentration of BNPs | Concentration of GNPs | Hydrodynamic diameter | Zeta potential |
| --- | --- | --- | --- | --- |
|  | [mg L-1] | [mg L-1] | (nm) | (mV) |
| 1 | 0 | 0 | 244.5 ± 31.0 | -20.9 ± 1.5 |
| 1 | 4 | 0 | 764.5 ± 63.1 | -21.7 ± 0.5 |
| 1 | 0 | 4 | 1089.4 ± 90.8 | -15.9± 0.8 |
| 0 | 4 | 0 | 398.6 ± 30.2 | -16.6 ± 0.9 |
| 0 | 0 | 4 | 348.8 ± 14.5 | 27.2 ± 1.2 |

Table S2. Other fitted model parameters.

| Model | Disp. | kdC | kdS |
| --- | --- | --- | --- |
|  | [-] | [min-1] | [min-1] |
| Co (MWCNTs) = 1 mg L-1, Co (BNPs/GNPs) = 0 mg L-1, 1 mM CaCl2 |  |  |  |
| M1 | 0.1171 | 0.0002 | NF |
| Co (MWCNTs) = 0 mg L-1, Co (BNPs) = 4 mg L-1, 1 mM CaCl2 |  |  |  |
| M1 | 0.01772 | NF | 0.001 |
| Co (MWCNTs) = 0 mg L-1, Co (GNPs) = 4 mg L-1, 1 mM CaCl2 |  |  |  |
| M1 | 0.01094 | NF | 0.001 |
| Co (MWCNTs) = 1 mg L-1, Co (BNPs) = 4 mg L-1, 1 mM CaCl2 |  |  |  |
| M1 | 0.332 | 0.0002 | 0.001347 |
| M2 | 0.332 | 0.0002 | 0.001347 |
| M3 | 0.332 | 0.0002 | 0.001347 |
| Co (MWCNTs) = 1 mg L-1, Co (GNPs) = 4 mg L-1, 1 mM CaCl2 |  |  |  |
| M1 | 0.01321 | 0.0002 | 0.002 |
| M2 | 0.01321 | 0.0002 | 0.002 |
| M3 | 0.01321 | 0.0002 | 0.002 |
| Co (MWCNTs) = 1 mg L-1, Co (BNPs/GNPs) = 0 mg L-1, 1 mM KCl |  |  |  |
| M1 | 0.1692 | 0.001 | NF |
| Co (MWCNTs) = 0 mg L-1, Co (BNPs) = 4 mg L-1, 1 mM KCl |  |  |  |
| M1 | 0.05346 | NF | 0.001 |
| Co (MWCNTs) = 0 mg L-1, Co (GNPs) = 4 mg L-1, 1 mM KCl |  |  |  |
| M1 | 0.0661 | NF | 0.002 |
| Co (MWCNTs) = 1 mg L-1, Co (BNPs) = 4 mg L-1, 1 mM KCl |  |  |  |
| M1 | 0.109 | 0.001 | 0.001 |
| M2 | 0.109 | 0.001 | 0.001 |
| M3 | 0.109 | 0.001 | 0.001 |
| Co (MWCNTs) = 1 mg L-1, Co (GNPs) = 4 mg L-1, 1 mM KCl |  |  |  |
| M1 | 0.05087 | 0.0005 | 0.008205 |
| M2 | 0.05087 | 0.0005 | 0.008205 |
| M3 | 0.05087 | 0.0005 | 0.008205 |

Disp. is the dispersion coefficient for the column experiments. kdC and kdS are the first-order release rate coefficient of MWCNTs, and of BNPs or GNPs, respectively.

Table S3. Standard error coefficients of fitted model parameters.

| Model | SCmax/Co | S.E. | ΓC | S.E. | kaC | S.E. | SSmax/Co | S.E. | ΓS | S.E. | kaS | S.E. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | [cm3g-1] | SCmax/Co | [-] | ΓC | [min-1] | kaC | [cm3g-1] | SSmax/Co | [-] | ΓS | [min-1] | kaS |
| Co (MWCNTs)=1 mg L-1, Co (BNPs/GNPs)=0 mg L-1, 1 mM CaCl2 |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | 2.752 | 0.167 | NF | NF | 62.91 | 1.860 | NF | NF | NF | NF | NF | NF |
| Co (MWCNTs)=0 mg L-1, Co (BNPs)=4 mg L-1, 1 mM CaCl2 |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | NF | NF | NF | NF | NF | NF | 2.603 | 0.065 | NF | NF | 30.16 | 1.880 |
| Co (MWCNTs)=0 mg L-1, Co (GNPs)=4 mg L-1, 1 mM CaCl2 |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | NF | NF | NF | NF | NF | NF | 3.294 | 0.118 | NF | NF | 45 | 6.179 |
| Co (MWCNTs)=1 mg L-1, Co (BNPs)=4 mg L-1, 1 mM CaCl2 |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | 2.322 | 0.050 | NF | NF | 56.32 | 0.851 | 2.553 | 0.159 | NF | NF | 22.98 | 2.198 |
| M2 | 2.322 | NF | 4.63E-02 | 0.234 | 56.32 | NF | 2.553 | NF | 5.88E-02 | 2.037 | 22.98 | NF |
| M3 | 1.37 | 1.639 | NF | NF | 1.06 | 0.856 | 0.939 | 0.095 | NF | NF | 0.591 | 0.069 |
| Co (MWCNTs)=1 mg L-1, Co (GNPs)=4 mg L-1, 1 mM CaCl2 |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | 3.153 | 0.134 | NF | NF | 63.98 | 17.762 | 3.051 | 0.398 | NF | NF | 29.14 | 8.080 |
| M2 | 3.153 | NF | 0.21 | 0.379 | 63.98 | NF | 3.051 | NF | 0.12 | 4.948 | 29.14 | NF |
| M3 | 6.113 | 271.17 | NF | NF | 1.107 | 4.245 | 1.493 | 0.395 | NF | NF | 0.687 | 0.101 |
| Co (MWCNTs)=1 mg L-1, Co (BNPs/GNPs)=0 mg L-1, 1 mM KCl |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | 1.621 | 0.059 | NF | NF | 16.47 | 0.335 | NF | NF | NF | NF | NF | NF |
| Co (MWCNTs)=0 mg L-1, Co (BNPs)=4 mg L-1, 1 mM KCl |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | NF | NF | NF | NF | NF | NF | 1.724 | 0.127 | NF | NF | 11.8 | 0.462 |
| Co (MWCNTs)=0 mg L-1, Co (GNPs)=4 mg L-1, 1 mM KCl |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | NF | NF | NF | NF | NF | NF | 2.796 | 2.070 | NF | NF | 22.76 | 7.709 |
| Co (MWCNTs)=1 mg L-1, Co (BNPs)=4 mg L-1, 1 mM KCl |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | 1.354 | 0.194 | NF | NF | 15.19 | 1.573 | 1.397 | 0.353 | NF | NF | 11.08 | 1.707 |
| M2 | 1.354 | NF | 1.95E-04 | 0.150 | 15.19 | NF | 1.397 | NF | 6.48E-04 | 0.161 | 11.08 | NF |
| M3 | 0.822 | 0.075 | NF | NF | 0.373 | 0.040 | 0.706 | 0.352 | NF | NF | 0.34 | 0.230 |
| Co (MWCNTs)=1 mg L-1, Co (GNPs)=4 mg L-1, 1 mM KCl |  |  |  |  |  |  |  |  |  |  |  |  |
| M1 | 1.733 | 0.400 | NF | NF | 39.07 | 6.502 | 2.08 | 0.547 | NF | NF | 13.92 | 1.897 |
| M2 | 1.733 | NF | 4.92E-02 | 0.124 | 39.07 | NF | 2.08 | NF | 1.56E-03 | 0.417 | 13.92 | NF |
| M3 | 1.271 | 0.887 | NF | NF | 0.82 | 0.410 | 0.945 | 0.097 | NF | NF | 0.41 | 0.004 |

S.E. is the standard error coefficient for each fitted parameter.

Fig. S1. Batch experiments under quasi-equilibrium conditions of MWCNTs on BNPs or GNPs in CaCl2 solution at an ionic strength of 1 mM.

Fig. S2. Plots of the dimensionless interaction energy as a function of separation distance (h) when a spherical colloid, with properties similar to MWCNTs in QS at an ionic strength of 1 mM CaCl2 or KCl in the presence or absence of BNPs or GNPs. (a) 1 mg L-1 MWCNT with adding 0 and 4 mg L-1 of BNPs or GNPs in 1 mM CaCl2 in QS; (b) 4 mg L-1 of BNPs or GNPs without MWCNTs in 1 mM CaCl2 in QS; (c) MWCNTs in the presence or absence of BNPs or GNPs in 1 mM CaCl2; (d) 1 mg L-1 MWCNT with adding 0 and 4 mg L-1 of BNPs in 1 mM KCl or CaCl2 in QS; (e) 1 mg L-1 MWCNT with adding 0 and 4 mg L-1 of GNPs in 1 mM KCl or CaCl2 in QS.

Fig. S3. Δf of MWCNTs (1 mg L-1), BNPs (4 mg L-1), and GNPs (4 mg L-1) in 1 mM CaCl2 (a) or KCl (b); ΔD/Δf of MWCNTs (1 mg L-1), BNPs (4 mg L-1), and GNPs (4 mg L-1) in 1 mM CaCl2 (c) or KCl (d); ΔD/Δf of MWCNTs (1 mg L-1) in the presence of BNPs (e) or GNPs (f) (4 mg L-1) in 1 mM KCl.

Fig. S4. Observed and fitted (M2) BTCs (a, c, e, and g) and RPs (b, d, f, and h) of MWCNTs, BNPs, and GNPs in quartz sand. (a) BTCs and (b) RPs of MWCNTs with adding 0 and 4 mg L-1 of BNPs or GNPs in 1 mM CaCl2; (c) BTCs and (d) RPs of BNPs or GNPs with adding 0 and 1 mg L-1 of MWCNTs in 1 mM CaCl2; (e) BTCs and (f) RPs of MWCNTs with adding 0 and 4 mg L-1 of BNPs or GNPs in 1 mM KCl; (g) BTCs and (h) RPs of BNPs or GNPs with adding 0 and 1 mg L-1 of MWCNTs in 1 mM KCl.

Fig. S5. Observed and fitted (M3) BTCs (a, c, e, and g) and RPs (b, d, f, and h) of MWCNTs, BNPs, and GNPs in quartz sand. (a) BTCs and (b) RPs of MWCNTs with adding 0 and 4 mg L-1 of BNPs or GNPs in 1 mM CaCl2; (c) BTCs and (d) RPs of BNPs or GNPs with adding 0 and 1 mg L-1 of MWCNTs in 1 mM CaCl2; (e) BTCs and (f) RPs of MWCNTs with adding 0 and 4 mg L-1 of BNPs or GNPs in 1 mM KCl; (g) BTCs and (h) RPs of BNPs or GNPs with adding 0 and 1 mg L-1 of MWCNTs in 1 mM KCl.

Fig. S6. Mass ratios (a) of retained MWCNTs due to retained BNPs or GNPs in co-transport experiments.

Fig. S7. Batch experiments of Ca2+ (IS = 1 mM) onto MWCNTs (1 mg L-1), BNPs (4 mg L-1), and GNPs (4 mg L-1) in Milli-Q water.