## Slide 1
HZO
TiN
NiSi2
NiSi2
Si
SiO2
Bulk Si
VPRO
Pre-Synaptic Neuron
Post-Synaptic Neuron
EPSC
Synapses with Homo/Hetero-Synaptic Plasticity Enabled by Ferroelectric Polarization Modulated Schottky Diodes
Andreas Grenmyr, Jiayuan Zhang, Stefan Wiefels, Detlev Grützmacher, Qing-Tai Zhao
Peter Grünberg Institute (PGI), Forschungszentrum Jülich, 52428 Jülich, Germany
[3] F. Xi et al, ESSCIRC 2022- IEEE, Milan, Italy, 2022, pp. 121-124.
Homosynaptic Fe-SBFET
Heterosynaptic Fe-SBFET
Single Synapses
Three-terminal Fe-SBFET
Holes or electrons as a neurotransmitter for the three-terminal Fe-SBFET.
Using the four-terminal Fe-SBFET, the input on the two gates can function as an AND logical gate, with the drain current as the output.
By having different configurations on the input, certain cells can be selected for highest weight.
Fe-SBFETs with three or four terminals have been fabricated, with excellent synaptic properties. The three-terminal device have ambipolar properties and therefore the synapse have two different neurotransmitters. Meanwhile, the four-terminal device can work as a heterosynaptic device with more conductive states.
By using the properties of Fe-SBFETs, both in memory logic, synapse arrays and integrate-and-fire neurons have been fabricated. This together with the CMOS compatible process for fabricating the Fe-SBFETs makes it highly relevant for the field of neuromorphic computing.
Neuromorpic Computing using CMOS compatible devices and technology promises high integration.
Heterosynaptic properties of the synapses are useful for achieving more conductive states.
HZO
TiN
NiSi2
NiSi2
Si
SiO2
Bulk Si
VMOD
Pre-Synaptic Neuron
Modulatory Neuron
VPRO
Post-Synaptic Neuron
EPSC
1
1
1
1
1
1
1
1
1
1
1
1
0
0
1
0
0
1
0
0
0
0
0
0
0
0
1
For a full neuromorphic system, both synapse arrays and neurons are required.
In this work, we present both synapses and neurons by using Fe-SBFETs on SOI with very simple structures.
VD= 1.0 V
+0.3V
-0.5V
0.5µs
0.5µs
0.5µs
0.5µs
-0.3V
1.0µs
1.0µs
1.0µs
1.0µs
VD= -0.3V
VMOD = -1.0 V
VMOD = 0.0 V
VD= -0.3V
+0.5V
-0.3V
1.0µs
1.0µs
1.0µs
1.0µs
+0.5V
G
G
SL 2
SL 1
WL1
WL2
BL 1
BL 2
(1,1)
(2,1)
(1,2)
(2,2)
VD= -0.1V
Reset
Fire
Integration
Fire
Self-Reset
Four-terminal Fe-SBFET
PPF using either holes or electrons as neurotransmitter for the three-terminal Fe-SBFET.
Holes as Neurotransmitter
Electrons as Neurotransmitter
Transfer curve of the three-terminal Fe-SBFET.
Synapse Arrays and Neurons
LTP/LTD curves for the three-terminal Fe-SBFET using either holes or electrons as a neurotransmitter.
LTP/LTD curves for the four-terminal Fe-SBFET with different modulation voltage applied, thereby changing the conductance.
[1] F. Xi et al, ACS Applied Materials & Interfaces 2021 13 (27), 32005-32012
If two inverters from the ambipolar Fe-SBFET are connected in series, they can work as an integrate- and-fire neuron.
TEM-image of a scaled down version of the Fe-SBFET with a gate lenght of 100nm.
FeFET
(2,1)
(2,2)
(2,1)
(1,1)
Selected Cell:
Design & Concept
Short-Term Plasticity
In Memory-Logic
Synapse Array
Neuron
References
Transfer Curve
Summary
Long-Term Plasticity
Holes as neurotransmitter
+0.5V
0.5µs
0.5µs
0.5µs
0.5µs
VD= 1.0V
-0.3V
Electrons as neurotransmitter
Scaled 100nm Fe-SBFET
Transfer curve of the four-terminal Fe-SBFET.
[2] Xi, F,. et al, Adv. Electron. Mater. 2023, 9, 2201155.
Acknowledgements
This work was partially supported by the Federal Ministry of Education and Research (BMBF, Germany) in the project NEUROTEC (16ME0398K).
Electrons as neurotransmitter
Holes as neurotransmitter
Input
VRead
Inverter 2
IRead
FeFET
VDD
Inverter 1
Inverter