## Slide 1: the Symbiotic Relationship between Ionomer and Water in Catalysts of PEM Fuel Cells
March 21, 2023 I Thomas Kadyk Theory and Computation of Energy Materials (IEK-13), Forschungszentrum Jülich

## Slide 2: What can be learned from existing models? Rationalize wetting behaviour in CCL Importance of cross-component coupling Open Access Modeling Platform

## Slide 3: Why theory and computation?
technology needs

## Slide 4: Why theory and computation?
technology needs
functional materials
ionic
catalytic
electronic
Molecular &
atomistic design
Notes: Talking about specific energy technology and understanding their use requirements a set of technology needs can be formulated, usually associated with power performance, storage capacity, economic viability or cost
Technology needs known, materials chemist or engineers can go to work to impart desired function into catalytic materials, ionic media, …,
however, rarely a simple correlation between materials structure and properties on the one hand and device level properties and opration can be drawn…

## Slide 5: Why theory and computation?
Composites & porous media
Structured materials
& interfaces
2D materials
(doping)
nanotemplated metals & alloys
metal oxides
oxynitrides
polymer/
ionomer networks
nanoprotonics/-ionics
transport media
mixed conductors
multiphase composites
ionic
catalytic
electronic
Molecular &
atomistic design
Notes: Form structured materials, modified environment and function, complex structures and local reaction conditions in composites and porous transport media
Maybe main challange is not to make a highly performing catalytic or ionic material but to sorround it with a well designed porous medium

## Slide 6: Why theory and computation?
Composites & porous media
Structured materials
& interfaces
Molecular &
atomistic design
2D materials
(doping)
nanotemplated metals & alloys
metal oxides
oxynitrides
polymer/
ionomer networks
nanoprotonics/-ionics
transport media
mixed conductors
multiphase composites
ionic
catalytic
electronic
DEVICE LEVEL  do properties meet use-specific demands?
MACROSCALE  mixed (“multi”) functionality
MESOSCALE  interfacial phenomena
MICROSCALE  transfer of energy, charge, and matter
INTRINSIC  mechanical, thermal, electronic, ionic, electrostatic, catalytic etc.
METRICS
DESCRIPTORS
Notes: Pick up descriptors while moving along structural hierarchy, become more complex (from simple adsorption energy where established and efficient tools to calculate to complex reaction conditions… )
level of sophistication, complexity of tools
Identifying viable descriptors or feature vectors and relating them to metrics of performance, lifetime, cost is main task of AI-driven materials design
Depending on depth of problem and complexity of tools: different level of maturity of AI concept

## Slide 7
interfaces
pores
mesostructures
DFT
DFT + micro-
kinetic modeling
DFT, AIMD,
CSM, DL theory
cMD, MF theory,
electrokinetics
CGMD, MF th.,
fluid dynamics
materials
nanostructures
components to devices
percolation, MHM,
fluid dynamics
Integration across scales
basic properties & interactions
transformations
potential distribution
local pH, ion conc.
effectiveness
performance & lifetime

## Slide 8
interfaces
pores
mesostructures
DFT
DFT + micro-
kinetic modeling
DFT, AIMD,
CSM, DL theory
cMD, MF theory,
electrokinetics
CGMD, MF th.,
fluid dynamics
materials
nanostructures
components to devices
percolation, MHM,
fluid dynamics
Integration across scales
basic properties & interactions
transformations
potential distribution
local pH, ion conc.
effectiveness
performance & lifetime
Piotr
Kowalski
Computational Materials Modeling
Artificial Materials Intelligence
Thomas Kadyk
Michael Eikerling
Physical Modeling and Diagnostics
Theory of EC Interfaces & Materials
Kourosh Malek
Young Invest. Group: EDL in Electrocatalysis

## Slide 9: Structure-based modeling of cathode catalyst Layers in PEM Fuel cells
Notes: Must understand local reaction conditions! Explain – next slide…

## Slide 10: From composition to effective properties
Primary parameters
component densities:
weight fractions:
Pt mass loading:
layer thickness:
per geometric surface area

## Slide 11: From composition to effective properties
Primary parameters:
component densities:
weight fractions:
Pt mass loading:
layer thickness:
per geometric surface area
Volumetric composition

## Slide 12: From composition to effective properties
Primary parameters
component densities:
weight fractions:
Pt mass loading:
layer thickness:
per geometric surface area
Volumetric composition
Effective properties from percolation theory
,
,

## Slide 13: Coupled species fluxes in CCLs

## Slide 14: Macrohomogeneous catalyst layer model
Part A: Governing equations for electrochemical processes
Part B: Governing equations for water fluxes
Proton transport
Vaporization
exchange
Vapour diffusion
Interfacial
reaction
Oxygen diffusion
Liquid transport
Water formation
and vaporization
One free parameter: j0
Problem: this part has two free parameters (total water flux, fraction of liquid flux)
 requires full MEA model
Polymer Electrolyte Fuel Cells – Physical Principles of Materials and Operation, M. Eikerling and A.A. Kulikovsky, CRC Press, 2014.

## Slide 15: MHM: Coupling
Part A: Governing equations for electrochemical processes
Part B: Governing equations for water fluxes
Proton transport
Vaporization
exchange
Vapour diffusion
Interfacial
reaction
Oxygen diffusion
Liquid transport
Water formation
and vaporization
explicit
coupling
Problem: implicit coupling –
dependence of solution on S(x)
Polymer Electrolyte Fuel Cells – Physical Principles of Materials and Operation, M. Eikerling and A.A. Kulikovsky, CRC Press, 2014.

## Slide 16: What harm can a flooded CCL possibly do?
important impact: thickness, composition, pore size distribution, wettability
assumption of constant composition sufficient below transition region
CCL flooding: important, but not critical! A flooded electrode could still perform well.

## Slide 17: Modeling Microstructure formation and wettability effects in Catalyst layers
Wolfgang
Notes: Must understand local reaction conditions! Explain – next slide…

## Slide 18: Modeling microstructure formation in CCL
support
ionomer
catalyst
Prediction of volumetric composition and ionomer film thickness and coverage based on ink recipe
CCL structure
~ 100 nm
T. Soboleva, PhD Thesis, Simon Fraser University, 2010.
Example: evolution of pore size distribution and porosity
ink composition (Pt:C, I:C)
specific materials properties
dispersion medium
fabrication conditions
Ink recipe & fab conditions
volume fractions (percolation)
pore size distribution
wettability (distribution)
interface areas and activity
transport properties
Notes: Three crucial ingredients that influence surface properties (and bulk)

## Slide 19: microstructure formation model: results
Basic correlations of ink parameters with CCL structure
A
C
B
Exp. data: T. Soboleva., PhD thesis, Simon Fraser University, 2010.
volume expansion
W. Olbrich et al., Electrochim. Acta 431, 140850.

## Slide 20: Wettability model: role of ionomer
Orientation of ionomer sidechains is the key (surface-induced ionomer inversion effect)
SO3-
SO3-
SO3-
SO3-
F
F
F
F
F
F
F
F
F
F
F
F
F
F
F
F
F
F
Hydrophilic ionomer surface
SO3-
SO3-
SO3-
SO3-
Hydrophobic ionomer surface
SO3-
SO3-
SO3-
SO3-
Ionomer inversion
earlier MD simulations
experimental studies
HO surface
HI surface
K. Malek et al. (2011). Electrocatalysis 2, 141-157.
Yu. M. Vol’fkovich et al. (2010). Russ. J. Electrochem. 438, 46.
quantitative analytical model

## Slide 21: Inversion mechanism based on Vol’fkovich data
W. Olbrich et al. (2022). J. Electrochem. Soc. 169, 054521.

## Slide 22: Wettability model
Stochastic process to generate heterogeneously wetted surfaces
ionomer (chunks of fixed size, rion ~ 5 nm) distributed randomly in secondary pore space
heterogeneous ionomer coverage → contact angle distribution (CAD)
Obtain water retention curve by integration over pore size distribution (PSD), contact angle distribution (CAD) and Young-Laplace criterion (YLP):
rion
Bernoulli process
n = trials p = chance
W. Olbrich et al., Electrochim. Acta 431, 140850.
Notes: YPL: flooded or not - Heaviside

## Slide 23: Wettability model: results
Pore size and contact angle distribution
-105 Pa
-104 Pa
(2)
(1)
-106 Pa
Combined PSD & CAD
(1) Hydrophilic primary pores and Pt-free nanopores
(2) Secondary pores with mixed wettability
-107 Pa
Contact angle distribution (secondary pores)
ionomer content
Pt content
dispersion param
W. Olbrich et al., Electrochim. Acta 431, 140850.

## Slide 24: Wettability model: water retention curves
H. P. F. Gunterman, PhD thesis, UC Berkeley, 2011.
Parametric effects
Comparison to experiment
W. Olbrich et al., Electrochim. Acta 431, 140850.

## Slide 25: Wettability Model: ccl optimization
Materials selection, modification, and design: tune parameters for optimal wettability distribution
fraction of hydrophobic secondary pore volume
kA = 4.5, Pt:C = 0.4
reducing Pt loading can tip the water balance (as seen earlier)
lower Pt loading: ionomer content must be more finely tuned
support modification → less sensitive to Pt and ionomer loading
W. Olbrich et al., Electrochim. Acta 431, 140850.

## Slide 26: Modeling Liquid Water Accumulation in Pem Fuel cell Cathode
D
M
CL
…
…
Yufan
Notes: Must understand local reaction conditions! Explain – next slide…

## Slide 27: Account for cross component coupling
Comprehensive model for water balance in cathode CL and DM
Solution space: pressure distribution → liquid saturation, fluxes

## Slide 28: Model assumptions
FF
cathode side: CL & DM and DM-FF interface
transport of oxygen (air), liquid and vapor water
one-dimensional
macrohomogeneous
isothermal
C
L
D
M
diffusion
diffusion
O2
liquid
vapor
diffusion
diffusion
vaporization
reaction
permeation
permeation
vaporization

## Slide 29: Pore size distributions and water retention curves
DM HO
CL HI
CL HO
CL HI
CL HO
DM HO
At the same , in CL and in DM are different.

## Slide 30: results
CL
GDL
Liquid saturation:
does not change much in CCL with j
GDL: formation of water layer at CL|GDL above jc
O2 diffusivity:
water layer causes abrupt decrease in diffusivity (to residual value)
O2 partial pressure:
drops drastically above jc before even reaching the CCL

## Slide 31: How to suppress water layer formation?
Tune the water retention curve: pore size distribution or contact angle
Strategies
smaller HO pores
larger contact angle
Water retention curve matters!

## Slide 32: How to suppress water layer formation?
Introducing another porous layer, the MPL!
K. Totaka et al. (2014). ECS Trans. 64, 839.
Underlying correlations

## Slide 33: Open Access Modeling Platform
Datum I Name
Subline der Präsentation bei umfänglicher Erläuterung

## Slide 34: Open Access Modeling Platform

## Slide 35: Open Access Modeling Platform
share models, tools and method
foster collaboration
enable others to use (and expand) our knowledge
provoke feedback
avoid redundant work
create visibility
Objectives

## Slide 36: Open Access Modeling Platform
Modular Model Implementation
  modules for governing equations, kinetics, parameters, diagnostic and analysis tools (Polcurve, EIS, CV, curr./volt. steps)
  allows restricting access to parts of the model -> allows using the platform for industry projects
Collaborative Programming Environment (GitLab etc.)
Modus Operandi

## Slide 37: Open Access Modeling Platform
Users
want to apply the model (e.g. Expermentalists)
need easy use (GUI, no need to install software, runs on server)
„Customers“
Developers
want to modify/contribute to the model (Modelers)
need easy understanding (documentation, programming language)
need collaborative environment (Gitlab, guidance/structure)
need exchange with other modelers (chat, meetings, workshops)

## Slide 38: Summary
energy materials design: a hierarchical challenge
role of ionomer on water retention in catalysts
interfaces between components

## Slide 39: Backup

## Slide 40
interfaces
pores
mesostructures
DFT
DFT + micro-
kinetic modeling
DFT, AIMD,
CSM, DL theory
cMD, MF theory,
electrokinetics
CGMD, MF th.,
fluid dynamics
materials
nanostructures
components to devices
percolation, MHM,
fluid dynamics
How to select or design materials?
basic properties & interactions
transformations
potential distribution
performance & lifetime
electronic structure,
adsorption energies, …
support properties,
particle density, …
interface properties,
local pH, …
effectiveness
local pH, ion conc.
pore geometry, …
ionomer & water distrib., …
thickness, composition

## Slide 41
interfaces
pores
mesostructures
DFT
DFT + micro-
kinetic modeling
DFT, AIMD,
CSM, DL theory
cMD, MF theory,
electrokinetics
CGMD, MF th.,
fluid dynamics
materials
nanostructures
components to devices
percolation, MHM,
fluid dynamics
How to select or design materials?
Intrinsic properties (usual suspects)
Set of structural and geometric parameters
Local reaction environment and rate determining term (set of parameters)
Fabrication and structure formation → properties
Cross-component coupling and response to ext. cond.

## Slide 42
interfaces
pores
mesostructures
DFT
DFT + micro-
kinetic modeling
DFT, AIMD,
CSM, DL theory
cMD, MF theory,
electrokinetics
CGMD, MF th.,
fluid dynamics
materials
nanostructures
components to devices
percolation, MHM,
fluid dynamics
Coupled reaction and transport (lifetime-performance, prospects and reserves for impovement)
Local reaction environment (charging relation, activity, stability and cat. utilization)
Intrinsic properties (electronic structure, rxn mechanisms, and rates)
How to select or design materials?

## Slide 43: Experimental Pore size distributions
T. Suzuki et al., Int. J. Hydrogen Energy, 36, 12361 (2011).
T. Soboleva et al., ACS AMI, 2, 375 (2010).
bimodal pores size distribution ( agglomeration)
hydrophobic and hydrophilic pores

## Slide 44: Modeling microstructure formation in CCL
Prediction of volumetric composition and ionomer film thickness and coverage based on ink recipe
Model: Piecewise self-assembly of ionomer during fabrication
Key parameter (descriptor): ionomer dispersion parameter, kA
W. Olbrich et al., Electrochim. Acta 431, 140850.
Notes: Decrease of free volume of secondary pore space
Growth of ionomer coverage at surface in secondary pore space
x: ratio of dry ionomer volume to volume of seconary pore space in ionomer-free sample
Film thickness: ratio of film volume to surface area covered

## Slide 45: Wettability Model
Alignment of ionomer sidechains
preferential ionomer sidechain orientation alters wettability in secondary pore space
depends on chemical nature of surface and interaction with ionomer constituents
Pt particles: help align sidechains towards support surface
Definition: degree of alignment, ΔDA,
W. Olbrich et al., Electrochim. Acta 431, 140850.
Notes: First equationlinear interpolation between surface area contributions
Third equation linear interplation
Fourth equation: mixing at surface
Second equation decay of alignment

## Slide 46: Effective properties as fuNCtion of liquid sat
vapor
(b) DM
(c) CL
(d) DM
HI HO
GDL
HI
HO
HO
vapor
(a) CL