## Slide 1
Post-test analysis
Cell preparation
Processing and durability of fuel electrode supported-cells with Ni-GDC electrode
Ni-GDC electrodes in fuel electrode-supported cells (FESC)
Electrochemical testing
Modelling of stress distribution: synthetic microstructures
NiO-YSZ support
Tape casting
NiO-GDC fuel electrode
Screen printing
GDC / YSZ / GDC electrolyte
Screen printing
Sintered half cell
1230 °C
1400 °C
1000 °C
NiO-YSZ support
Tape casting
NiO-GDC fuel electrode
Screen printing
GDC electrolyte
Screen printing
Sintered half cell
1230 °C
850 °C
1400 °C
8YSZ layer (PVD)
GDC layer (PVD)
LSC air electrode
Screen printing
1000 °C
80% pH2O 5%
10 µm
LSC
GDC
Ni-GDC
Ni-YSZ
Microstructural parameter | Material | 0 h | 1100 h | 2000 h
Volume fraction FE (%) | CGO | 49 | 51 | 50
 | Pores | 22 | 21 | 21
 | Ni | 29 | 28 | 29
Tortuosity | Pores (FE) | 4.9 | 4.5 | 4.4
 | Ni | 4.5 | 5.7 | 4.8
Area/Volume () | Ni | 0.01 | 0.009 | 0.01
TPB/Vol Electrode () |  | 0.04 | 0.08 | 0.05
Microstructural parameter | Material | 0 h | 1100 h | 2000 h
Volume fraction FE (%) | CGO | 49 | 51 | 50
 | Pores | 22 | 21 | 21
 | Ni | 29 | 28 | 29
Tortuosity | Pores (FE) | 4.9 | 4.5 | 4.4
 | Ni | 4.5 | 5.7 | 4.8
 | Ni | 0.01 | 0.009 | 0.01
 |  | 0.04 | 0.08 | 0.05
Microstructure
GDC
GDC
YSZ
NiO GDC
NiO YSZ
Porosity 14 %
10 µm
Bimodal
Unimodal
GDC
YSZ
GDC
NiO GDC
NiO YSZ
Porosity 5 %
10 µm
Interface
Contrast inverted
Powder processing and interdiffusion
Physical vapor deposition (PVD) cells
Screen printing (SP) cells
Gd
Ce
Y
Zr
20 µm
5 µm
Chart: At%
2 µm
EDX analysis of TEM lamella
Chart: At%
| 0.13723694847332199 | 0.68618474236660498 | 1.2351325362598899 | 1.78408033015317 | 2.3330281240464501 | 2.8819759179397302 | 3.43092371183302 | 3.9798715057263001 | 4.5288192996195802 | 5.0777670935128603 | 5.6267148874061501 | 6.1756626812994302 | 6.7246104751927103 | 7.2735582690859903 | 7.8225060629792802 | 8.37145385687257 | 8.9204016507658395 | 9.4693494446591302 | 10.0182972385524 | 10.567245032445699 | 11.116192826339001 | 11.6651406202323 | 12.2140884141255 | 12.7630362080188 | 13.3119840019121 | 13.860931795805399 | 14.409879589698701 | 14.958827383592 | 15.5077751774852 | 16.056722971378498 | 16.6056707652718 | 17.154618559165101 | 17.703566353058399 | 18.2525141469517 | 18.801461940844899 | 19.3504097347382 | 19.899357528631501 | 20.448305322524799 | 20.997253116418101 | 21.546200910311299 | 22.0951487042046 | 22.644096498097898 | 23.1930442919912 | 23.741992085884501 | 24.290939879777799 | 24.839887673671001 | 25.388835467564299 | 25.9377832614576 | 26.486731055350901 | 27.035678849244199
Gd At% | 2.9058 | 2.8982 | 2.8473 | 2.8006 | 2.8782 | 2.1076 | 1.4432 | 0.71321 | 0.34868 | 0.11349 | 0.075396 | 0.068292 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.0021413 | 0.0022304 | 0 | 0.020923 | 0 | 0.013796 | 0.37016 | 0.98461 | 1.835 | 2.7957 | 3.0132 | 3.0342 | 1.8245 | 3.1498 | 3.0823 | 3.0215
O At% | 67.8226 | 67.8325 | 67.5445 | 67.0482 | 66.2964 | 65.0722 | 65.2608 | 64.983 | 65.2642 | 65.4333 | 65.6058 | 65.4922 | 65.7508 | 65.5732 | 65.6101 | 65.6432 | 65.491 | 65.6638 | 65.1331 | 65.6166 | 65.2811 | 65.2474 | 65.8739 | 65.5517 | 65.8508 | 65.2693 | 65.7207 | 65.9958 | 65.4534 | 65.6332 | 65.7837 | 65.8184 | 65.5848 | 65.1962 | 65.2802 | 65.8295 | 65.7729 | 65.431 | 65.6073 | 65.4287 | 65.4072 | 65.2233 | 64.6238 | 65.0371 | 66.6889 | 67.1656 | 72.1133 | 67.9148 | 67.6793 | 68.1
Y At% | 0.10339 | 0.30695 | 0.41154 | 1.152 | 2.3601 | 6.0247 | 7.2872 | 8.288 | 8.4471 | 8.35 | 8.2825 | 8.5669 | 8.4748 | 8.4094 | 8.3479 | 8.5082 | 8.5627 | 8.7398 | 8.8731 | 8.5778 | 8.602 | 8.8416 | 8.4901 | 8.6106 | 8.5064 | 8.8469 | 8.7755 | 8.4459 | 8.6145 | 8.2893 | 8.3136 | 8.2487 | 8.7263 | 8.671 | 8.6657 | 8.2624 | 8.2289 | 8.2828 | 8.1725 | 8.224 | 7.8921 | 7.531 | 6.9185 | 4.1198 | 1.4498 | 0.64783 | 5.2445 | 0.40822 | 0.19397 | 0
Zr At% | 1.3118 | 2.3725 | 3.2852 | 5.0768 | 8.6634 | 16.6143 | 20.0401 | 21.9776 | 23.0897 | 23.9715 | 24.1984 | 24.4488 | 24.7486 | 25.0288 | 25.0532 | 25.0952 | 25.2927 | 25.1849 | 25.2903 | 25.2769 | 25.6037 | 25.3691 | 25.1224 | 25.3546 | 25.2394 | 25.219 | 24.8701 | 25.1476 | 25.3077 | 25.4472 | 25.3205 | 25.3735 | 25.1609 | 25.3238 | 25.2001 | 24.9956 | 24.9201 | 24.6604 | 24.3615 | 24.2174 | 22.9168 | 20.926 | 18.8013 | 13.5479 | 6.3284 | 3.6896 | 2.2651 | 1.1162 | 0.35551 | 0.38235
Ce At% | 27.8564 | 26.5898 | 25.9115 | 23.9223 | 19.802 | 10.1812 | 5.9687 | 4.0382 | 2.8503 | 2.1317 | 1.8379 | 1.4238 | 1.0259 | 0.98857 | 0.9889 | 0.7534 | 0.65362 | 0.41156 | 0.70352 | 0.52871 | 0.51326 | 0.54181 | 0.51367 | 0.4831 | 0.40343 | 0.6648 | 0.63377 | 0.41063 | 0.62439 | 0.63032 | 0.58218 | 0.55943 | 0.528 | 0.80898 | 0.85198 | 0.91025 | 1.0781 | 1.6049 | 1.8588 | 2.1161 | 3.4138 | 5.335 | 7.8214 | 14.4995 | 22.5196 | 25.4627 | 18.5526 | 27.411 | 28.689 | 28.4961
5 µm
O
Ce
Gd
Zr
Y
O
Ce
Gd
Zr
Y
GDC
YSZ
GDC
GDC
YSZ
GDC
GDC
YSZ
GDC
GDC
YSZ
GDC
604 mΩ cm²
176 mΩ cm²
151 mΩ cm²
~ 100 mΩ cm²
PVD
2-step
OCV + ASR
22 µm YSZ
4 µm YSZ
Optimization of processing
Monomodal PSD minimizes porosity
Powder pre-treatment to adjust shrinkage rate in co-fired layers
Optimization of binder + dispersant content
Influence of powder characteristics on the rheology of ceria-based screen-printing
Processing
Interdiffusion during co-sintering
PVD
SP cells
Electrochemical impedance spectroscopy
Electrochemical impedance spectroscopy
800 °C
Air / 50:50 H2:H2O
Re(Z) [Ωcm²]
Re(Z) [Ωcm²]
Im(Z) [Ωcm²]
Im(Z) [Ωcm²]
initial Time 560 h
Re(Z) [Ωcm²]
Re(Z) [Ωcm²]
Im(Z) [Ωcm²]
Im(Z) [Ωcm²]
800 °C
Air / 50:50 H2:H2O
-1.5 A cm-2
800 °C
Air / 50:50 H2:H2O
-1.5 A cm-2
Durability test (800 °C, 50:50 H2:H2O, -1.5 Acm-²)
Durability test (800 °C, 50:50 H2:H2O, -1.5 Acm-²)
Conclusions
Very low area-specific resistance (ASR)
Stable ASR during durability test
OCV lower than VNernst indicates gas / electronic leakage
Faradaic efficiency yet unknown (assumed < 100%)
Decreasing OCV indicates increasing leakage
Conclusions
High ASR (higher than SoA Ni-YSZ cells)
High degradation rate during stability test (esp. Rohm)
OCV = VNernst indicates no leakage
Faradaic efficiency yet unknown (assumed 100%)
Stable OCV during testing
R [Ωcm²]
R [mΩcm²]
Cell voltage [V]
Cell voltage [V]
T [°C]
T [°C]
Time [h]
Time [h]
Time [h]
Time [h]
PVD cells
PVD cells
Cracks found in the active area of the cell
No cracking next to the air electrode
Very little reoxidation indicates cracking during cooling
3D reconstruction by FIB-SEM shows no change in microstructural parameters after 2000 hours of SOEC operation
SP cells
10 µm
10 µm
Cell after reduction
Agglomerates in GDC layers
High porosity at the YSZ-GDC interfaces after sintering ( leads to high ohmic resistance due to low contact area)
Dense YSZ and GDC layers
Cell after SOEC operation
Cracks at regular intervals through GDC layer
YSZ layer mechanically intact ( stable OCV)
Strong delamination along YSZ-GDC co-sintered interface ( increasing ohmic resistance)
No indication of Ni depletion / migration despite high cell voltage
Generation of synthetic microstructures
Prediction of electro-chemo-mechanical stress
Material properties
Electrochemical data
Chemical expansion of GDC
Distribution of pO2
Stress prediction in synthetic microstructures
Acceleration compared to experiments: simple variation of microstructure – property relation
Requires accurate input parameters
Assumptions & boundary conditions critical
MPa
FIB-SEM 3D reconstruction
Generated microstructure
MPFM aging simulation
Microstructure variation
GDC, air
GDC, 4% H2
YSZ, 4% H2
YSZ, air
GDC
GDC
YSZ
800 °C
Air / 50:50 H2:H2O
80% pH2O 5%
initial Time 350 h
MPFM: Multiphase-field method