## Slide 1
Leaching mechanism = selective removal of cations
Still state-of-the art for waste management agencies but under debate in the scientific community
Dissolution of simplified nuclear waste glass (ISG) and
formation of secondary phases
Felix Brandt1, Martina Klinkenberg1 , Sébastien Caes2, Jenna Poonoosamy1, Wouter Van Renterghem3, Juri Barthel 4, Karel Lemmens2, Dirk Bosbach1, Karine Ferrand2
1Institute of Energy and Climate Research (IEK-6), Nuclear Waste Management and Reactor Safety, Forschungszentrum Jülich GmbH, 52425 Jülich, Germany; f.brandt@fz-juelich.de
2Institute for Environment, Health and Safety, SCK CEN, B-2400 Mol, Belgium; 3Institute for Microstructural and Non-Destructive Analysis, SCK CEN, B-2400 Mol, Belgium
4Ernst Ruska-Centre (ER-C 2), Forschungszentrum Jülich GmbH, 52425 Jülich, Germany
Introduction & Objectives:
Gin et al., 2013
SA/V ratio is a key parameter for the dissolution rate and the formation of the altered glass surface and secondary phases at high pH conditons.
Macroscopic element release NLi and residual dissolution rate of 6 x 10-6 g/m2d in a usual range
No resumption although secondary phases are formed
Thermodynamic blind predictions can predict the observed secondary phases, some phases are missing due to kinetic reasons
CSH phases and zeolites confirmed by SEM, XRD or TEM. Stable phases such as K-zeolite present as well as metastable Na-zeolite and CSH of a kinetically controlled composition.
The unusual microstructure: very thin, porous layer from which CSH phases appeared to have grown
 Competition between dissolution/re-precipitation of secondary phases and formation of a leached layer
Models based on the proposed leaching mechanism are mainly based on macroscopic experiments at low surface area to volume (SA/V) ratio (e.g. Frugier et al., 2018)
Details of surface alteration layer (SAL) formation?
Formation of new phases and incorporation of RN?
Relevant experimental conditions e.g. high pH, low T due to the presence of concrete and cement?
 The microscopic view
Thermodynamic equilibrium calculation based on mass balance of dissolved elements (NLi)
Blind prediction: All cations released end up in secondary phases, if they are supersaturated.
Macroscopic perspective
Normalized element release NLi = amount of glass (g/m2) dissolved at a given time calculated from the element release. NLi and residual rateof 6 x 10-6 g/m2d in the usual range
Results:
Predicted and observed
Zeolite
CSH (Okenite)
Not observed due to kinetics
Quartz
Baddeleyite
ISG
Batch experiments at high pH and high SA/V
Modelling of thermodynamic equilibria (GEMS-PSI)
Estimation of secondary phase equilibrium assuming congruent dissolution and precipitation
YCWCa
Characterization of the solid
Separation of crystalline secondary phases
XRD of separated grain size fractions
Electron microscopy: SEM, FIB, TEM
Sample taken from day 385
Sample embedded in resin
Polished to obtain a cross-section
FIB section prepared perpendicular to the polished surface
References:
Frugier, P. et al 2008. J. Nucl. Mater. 380, 8–21. DOI: 10.1016/j.jnucmat.2008.06.044
Gin, S. et al. 2013. Mater. Today 16, 243–248. DOI: 10.1016/j.mattod.2013.06.008
Mann, C. et al. 2019. npj Mater. Degrad. 3, 5. DOI: 10.1038/s41529-018-0059-9
Effect of high pH
Morphology and properties of altered phase?
Type of newly formed secondary phases?
Lower temperature
More difficult to form crystalline secondary phases?
Slower dissolution of the glass?
Higher SA/V
More secondary phase formation?
Summary and Conclusions:
Materials and Methods:
Microscopic perspective, residual stage:
the glass/SAL interface (TEM), SA/V = 264000 m-1
Very thin porous altered layer, no colloids
Structure resembles a bubble foam
Fibrous secondary phases
relationship with the cavities of the porous layer?
Identification of secondary phases (XRD + SEM)
Zeolites (Na and K zeolite)
Calcium silicate hydrate phases (CSH)
SA/V = 8300 m-1
Mann et al., 2019, ISG glass in YCWCa @70 °C
Gel layer of multiple colloidal bands
Sharp boundaries between layers
Crystalline phases formed around the outer edge
Mann et al., 2019
15 µm