Tape-cast Ce-substituted Li7La3Zr2O12 Electrolyte for Improving Electrochemical Performance of Solid-State Lithium Batteries

Purna Chandra Rath, Yu-Syuan Jheng, Cheng-Chia Chen, Chih-Long Tsai, Yu-Sheng Su, Chun-Chen Yang, Rüdiger-A. Eichel, Chien-Te Hsieh, Tai-Chou Lee, Jeng-Kuei Chang

Table S1.  Chemical composition of LLZO, LGLZO, and various LLZCO samples examined using ICP-MS.

| Sample | Chemical formula | Li | La | Zr | Ce | Ga |
| --- | --- | --- | --- | --- | --- | --- |
| LLZO | Li7La3Zr2O12 | 5.16 | 3.000 | 1.97 | NA | NA |
| LGLZO | Li6.25Ga0.25La3Zr2O12 | 4.18 | 3.000 | 2.00 | NA | 0.28 |
| LLZCO-0.05 | Li7La3Zr1.95Ce0.05O12 | 4.99 | 3.000 | 1.96 | 0.050 | NA |
| LLZCO-0.10 | Li7La3Zr1.90Ce0.10O12 | 5.02 | 3.000 | 1.90 | 0.095 | NA |
| LLZCO-0.15 | Li7La3Zr1.85Ce0.15O12 | 5.02 | 3.000 | 1.84 | 0.145 | NA |

Fig. S1. SEM images of (a) LLZCO-0.05 and (b) LLZCO-0.15 samples.

Fig. S2. DLS data of LLZO, LGLZO, and various LLZCO samples.

@0.1 C

Fig. S3. Charge-discharge curves of Li//CSE//LFP cell with 25 wt.% LGLZO and EO/Li+ molar ratio of 5 in CSE.

Fig. S4. (a) Charge-discharge curves of Li//LFP cell assembled with freestanding CSE. (b) Comparative rate performance of Li//LFP cells with freestanding and tape-cast CSE layers. (c) EIS spectra of Li//LFP cell assembled with freestanding CSE.

Fig. S5. (a) Cross-sectional SEM image of tape-cast CSE on LFP cathode. (b) The corresponding EDS Fe and S mapping in the same region.

Fig. S6. Charge-discharge curves of Li//CSE (with EO/Li+ = 10 and 35 wt.% LGLZO)//LFP cell with CSE thickness of (a) 20, (b) 50, and (c) 80 µm.

Fig. S7. Overpotential derived from charge-discharge curves (in Fig. 7) of Li//CSE//LFP cells with various  CSEs.

Fig. S8. SEM images of (a) LLZO (b) LLZCO-0.10 pellets after Li contact for 48 hours at 70 °C.

Fig. S9. Charge-discharge curves of Li//LLZCO-0.10 CSE//LFP cell measured at (a) 0.1 C and (b) 0.5 C at various temperatures.